HMQ-ES-Stack-GBR: Methodology, Data Generation, Results & Conclusion

Condensed version based on the associated paper and Mendeley dataset (Version 2)

# 1. Research Objective

The study develops a data-driven framework to predict and optimize the quality of FDM 3D-printed parts. It predicts five outputs—peak stress, strain at break, elastic modulus, hardness, and surface roughness—and then searches for suitable printing parameters for each material.

Overall workflow: Printing parameters → Physical specimens → Laboratory testing → Data cleaning → Machine-learning prediction → Validation → Feature importance → Multi-objective optimization.

# 2. Experimental Data Generation

| Component | Details |
| --- | --- |
| Materials | 10 polymers: PLA+, PETG, ABS, PLA-CF, TPU, PLA-phosphorus, PLA-transparent, PLA, rPET and PP |
| Parameters | Layer thickness: 0.1/0.2/0.3 mm; Infill: 20/50/80%; Speed: 30/50/70 mm/s; Pattern: Zigzag/Grid/Triangles |
| Printers | Creality Ender-3 Pro (open case) and Creality K1 (closed case) |
| Configurations | 500 distinct combinations |
| Replicates | 3 per configuration |
| Total specimens | 1,500 physical specimens |
| Specimen standard | ISO 527-2 Type 4 |

# 3. How the Output Data Were Generated

The dataset is based on physical experiments, not simulated outputs. Printed specimens were tested using standardized laboratory procedures.

| Test | Outputs |
| --- | --- |
| Tensile test | Peak stress, strain at break, elastic modulus |
| Hardness test | Shore D hardness |
| Surface roughness | Average roughness (Ra) |

IQR-based outlier detection and data-quality checks were performed. Repeatability was assessed using coefficient of variation. Validated replicates were averaged, producing 500 final experimental records from the original 1,500 specimens.

# 4. Machine-Learning Methodology

Several regression algorithms were benchmarked. XGBoost, Random Forest (RF), and Gradient Boosting Regressor (GBR) were selected as Level-0 models. Their predictions were combined using a Level-1 GBR meta-learner, forming HMQ-ES-Stack-GBR.

| Stage | Method |
| --- | --- |
| Level 0 | XGBoost + Random Forest + GBR |
| Intermediate | Out-of-Fold (OOF) predictions |
| Level 1 | GBR meta-learner |
| Outputs | Stress, strain, modulus, hardness, roughness |

Validation used an 80/20 development/hold-out split. Five-fold cross-validation was performed on the development portion, with OOF predictions used to train the meta-learner. The final model was evaluated on the untouched 20% test set.

# 5. Important Findings

Material type was the dominant feature, contributing approximately 55% of total feature importance. Layer thickness was next, while infill density and printer type had similar influence; printing speed was comparatively less important within the tested range.

Rigid materials such as PLA, PLA+ and PETG generally showed more stable predictions than highly deformable materials such as TPU and PP. Surface roughness was the most difficult output because its experimental variability was higher.

# 6. Model Results

| Target | R² | MAE | RMSE |
| --- | --- | --- | --- |
| Strain at break | 0.999 | 0.0006 | 0.0009 |
| Peak stress | 0.999 | 194.5932 kPa | 256.1791 kPa |
| Elastic modulus | 0.994 | 57.9000 MPa | 76.4403 MPa |
| Hardness | 0.991 | 1.0843 | 1.4143 |
| Surface roughness | 0.936 | 0.4058 µm | 0.5290 µm |

HMQ-ES-Stack-GBR outperformed the evaluated baseline models. The improvement was particularly noticeable for surface roughness, where the closest reported comparison achieved R² ≈ 0.733 versus 0.936 for the proposed model.

# 7. Optimization Methodology

The trained ML model was used as a surrogate model: it estimates the quality of candidate printing settings without physically printing every candidate. NSGA-II, Particle Swarm Optimization (PSO), and Grey Wolf Optimizer (GWO) were used.

Optimization was performed separately for each material. The objective was to minimize surface roughness while maximizing hardness, peak stress, strain at break and elastic modulus.

# 8. Key Limitations

Validation was mainly internal to the experimental dataset; independent external validation was not reported.

Material and printer groups were not perfectly balanced.

The very high R² values may warrant additional validation for possible overfitting.

Surface roughness had substantially higher experimental variability.

Generalization to unseen printers, materials, or parameter ranges remains to be established.

# 9. Conclusion

The study presents a complete experimental-to-machine-learning pipeline for FDM quality prediction using measured data from 1,500 physical specimens covering 10 materials, multiple process parameters and two printer configurations.

HMQ-ES-Stack-GBR combines XGBoost, Random Forest and GBR through two-level stacking and achieves very high predictive accuracy within the studied parameter range. NSGA-II, PSO and GWO then extend the framework from prediction to material-specific process optimization.

Overall, the framework is best viewed as a pre-print diagnostic and decision-support system. Further external validation is needed before claiming universal generalization to new materials, machines or industrial environments.

# 10. Methodology in One Flow

1. Ten polymer materials were selected, and the printing configurations were defined.
2. Four principal process parameters were used: layer thickness, infill density, printing speed, and infill pattern.
3. Print 500 unique configurations, with three physical replicates each → 1,500 specimens.
4. Standardised ISO 527-2 Type 4 specimen geometry was used.
5. Measure the tensile properties, hardness, and surface roughness using calibrated equipment.
6. Data quality control, IQR-based sanitisation, consistency checks, and replicate analyses were performed.
7. The average validated replicates were used to obtain 500 final experimental records.
8. The data were split into 80% development and 20% final hold-out testing.
9. Use 5-fold CV within the training portion to generate OOF predictions.
10. Benchmark multiple regression algorithms
11. Select XGBoost, Random Forest, and GBR as Level-0 base learners.
12. Train a GBR Level-1 meta-learner on OOF predictions → HMQ-ES-Stack-GBR.
13. Evaluate using R², MAE, RMSE, and residual/correlation analysis.
14. Analyse feature importance and material/printer-specific error patterns.
15. The trained predictor was used as a surrogate model inside the NSGA-II, PSO, and GWO optimisations.
16. Generate material-specific recommended process parameter combinations.

# Source

Aktepe, E. & Ergün, U. (2026). HMQ-ES-Stack-GBR: A Hybrid Ensemble Learning Model for Mechanical and Physical Quality Prediction in FDM 3D Printing. Micromachines, 17(7), 859. Dataset DOI: 10.17632/zd6td6svd6.2.